Caledonian Mining Cables

AS/NZS 1972:2006 Cables

Paper Insulated 11/11KV

� Applications .............................................................................................................

These cables are used as HV feeder cables in fixed conditions.

� Standards .................................................................................................................

AS/NZS 1972:2006

AS/NZS 1125

AS/NZS 3808

� Construction ............................................................................................................

Outer PVC Sheath

Shaped Stranded Copper Conductor Paper Insulation

Jute Filler

Paper Tape Belt Insulation Inner Lead Sheath

PVC Bedding

Galvanized Steel Wire Armour

Conductors: Sector shaped stranded copper conductor.

Insulation: Paper tape.

Filling: Jute fillers.

Insulation: Paper tape belt insulation.

Inner Sheath: Lead sheath.

Bedding: PVC sheath.

Armour: Galvanized steel wire armour.

Outer Sheath: PVC sheath to AS/NZS 1026.

www.caledonian-cables.co.uk  www.addison-cables.com	53

Caledonian Mining Cables

AS/NZS 1972:2006 Cables

�  Dimensions and Weight ..........................................................................................

| Nominal Conductor Area | Minimum Insulation Thickness | Nominal Lead Sheath Thickness | Armour Wire Diameter | Nominal Sheath Thickness | Nominal Overall Diameter | Nominal Weight |
| --- | --- | --- | --- | --- | --- | --- |
|  | Between Conductors | Between Conductors and Lead Sheath |  |  |  |  |  |
| mm� | mm | mm | mm | mm | mm | mm | kg/100m |
| 25 | 5.6 | 5.4 | 1.8 | 2.5 | 2.4 | 47.9 | 630 |
| 35 | 5.6 | 5.4 | 1.8 | 2.5 | 2.5 | 50.3 | 695 |
| 50 | 5.6 | 5.4 | 1.8 | 2.5 | 2.5 | 50.1 | 725 |
| 70 | 5.6 | 5.4 | 1.9 | 2.5 | 2.6 | 53.5 | 855 |
| 95 | 5.6 | 5.4 | 2.0 | 2.5 | 2.6 | 57.2 | 1000 |
| 120 | 5.6 | 5.4 | 2.0 | 2.5 | 2.7 | 60.1 | 1120 |
| 150 | 5.6 | 5.4 | 2.1 | 2.5 | 2.8 | 63.0 | 1260 |
| 185 | 5.6 | 5.4 | 2.3 | 3.15 | 2.9 | 68.0 | 1540 |
| 240 | 5.6 | 5.4 | 2.4 | 3.15 | 3.0 | 73.1 | 1820 |
| 300 | 5.6 | 5.4 | 2.6 | 3.15 | 3.2 | 77.9 | 2120 |
| 400 | 5.6 | 5.4 | 2.7 | 3.15 | 3.4 | 83.5 | 2500 |

54	www.caledonian-cables.co.uk  www.addison-cables.com