Caledonian Mining Cables

Portable Power Cables

Type G Two-Conductor Flat Portable Power Cable 2kV

� Applications .............................................................................................................

These ﬂat parallel cables are designed for use on D�C� oﬀ-track mining equipment, such as D�C� shuttle cars, drills, cutting and loading machines�

� Standards .................................................................................................................

ICEA S-75-381/NEMA WC 58 ASTM B 172

ASTM B 33

CAN/CSA-C22�2 No�96

� Construction ............................................................................................................

Stranded Tinned Copper Conductor EPR Insulation

Grounding Conductor

Synthetic Yarn Braid Renforcement CPE Jacket

Conductors:

Stranded annealed tinned copper conductor�

Insulation:

Ethylene Propylene Rubber (EPR)�

Grounding Conductor:

Tinned copper conductor with an optional green outer covering�

Reinforcement: Synthetic yarn� Jacket:

Heavy-duty/extra-heavy-duty Chlorinated Polyethylene (CPE), black� (Cables having a nominal outside diameter of more than 2�0 inches require extra-heavy-duty jackets�)

www.caledonian-cables.co.uk  www.addison-cables.com	15

Caledonian Mining Cables

Portable Power Cables

� Options .....................................................................................................................

Other jacket materials such as CSP/PCP/NBR/PVC are available upon request�

Two-layer jacket with reinforcing fibre between the two layers can be oﬀered  as an option�

�  Mechanical and Thermal Properties ......................................................................

Minimum Bending Radius: 6�OD

Maximum Conductor Operating Temperature: +90℃

�  Dimensions and Weight

.........................................................................................

| Construction | No. of Strands | Grounding Conductor Size | Nominal Insulation Thickness | Nominal Jacket Thickness | Nominal Overall Diameter Height譝idth | Nominal Weight | Ampacity |
| --- | --- | --- | --- | --- | --- | --- | --- |
| No. of cores� AWG/kcmil | - | AWG/ kcmil | inch | mm | inch | mm | inch | mm | lbs/kft | kg/km | A |
| 2�6 | 133 | 8 | 0�06 | 1�5 | 0�080 | 2�0 | 0�56�1�02 | 14�2�25�9 | 500 | 744 | 95 |
| 2�4 | 259 | 7 | 0�06 | 1�5 | 0�095 | 2�4 | 0�61�1�15 | 15�5�29�2 | 635 | 945 | 127 |
| 2�3 | 259 | 6 | 0�06 | 1�5 | 0�095 | 2�4 | 0�68�1�26 | 17�3�32�0 | 785 | 1170 | 145 |
| 2�2 | 259 | 5 | 0�06 | 1�5 | 0�095 | 2�4 | 0�73�1�35 | 18�5�34�3 | 935 | 1390 | 167 |
| 2�1 | 259 | 4 | 0�08 | 2�0 | 0�110 | 2�8 | 0�81�1�55 | 20�6�39�4 | 1185 | 1760 | 191 |
| 2�1/0 | 259 | 3 | 0�08 | 2�0 | 0�125 | 3�2 | 0�93�1�67 | 23�6�42�4 | 1470 | 2190 | 217 |
| 2�2/0 | 329 | 2 | 0�08 | 2�0 | 0�125 | 3�2 | 0�99�1�85 | 25�1�47�0 | 1790 | 2660 | 250 |
| 2�3/0 | 413 | 1 | 0�08 | 2�0 | 0�140 | 3�6 | 1�03�2�00 | 26�2�50�8 | 2145 | 3190 | 286 |
| 2�4/0 | 532 | 1/0 | 0�08 | 2�0 | 0�140 | 3�6 | 1�10�2�10 | 27�9�53�3 | 2545 | 3790 | 328 |

Ampacity-Based on a conductor temperature of 90℃ and an ambient air temperature of 40℃, per ICEA S-75-381�

16	www.caledonian-cables.co.uk  www.addison-cables.com