Caledonian Mining Cables Cables for Underground Mining

NTMTWOEU 0.6/1kV Mine Hoist Cables

�  Applications

These cables are used as suspended cable for intrinsically safe control of user-operated mine hoists (lifts) with telephonic connection in underground mines.

�  Standards

VDE 0250 Part 813

�  Construction

Stranded Tinned Copper Conductor 3GI3 Insulation

Shielded Telephone-type Pilot Steel Support Element

Textile Braid

5GM5 Outer Sheath

Conductors: Flexible stranded tinned copper conductor, class 5 according to DIN VDE 0295.

Insulation: EPR type 3GI3.

Support Element: Central steel support element.

Anti-torsion Braid: Textile braid.

Outer Sheath: PCP rubber type 5GM5.

�  Dimensions and Weight

| Number of Cores譔ominal Cross Section | Minimum Overall Diameter | Maximum Overall Diameter | Nominal Weight |
| --- | --- | --- | --- |
| No. 譵m� | mm | mm | kg/km |
| 8x2.5ST+2x1FM(C) | 21�7 | 23�7 | 800 |
| 8x2.5ST+10x (2x1FM)C | 34�0 | 37�5 | 1450 |
| 14x2.5ST+6x1FM(C) | 27�0 | 31�0 | 1200 |
| 18x2.5ST+6x1FM(C) | 38�0 | 42�0 | 1800 |
| 19x1.5(C)ST+6x (2x1FM)C | 35�1 | 38�1 | 2145 |

www.caledonian-cables.co.uk  www.addison-cables.com	13